SECTION 07 46 23

ENGINEERED WOOD SIDING

Display hidden notes to specifier. (Don't know how? Click Here)

Copyright 2019 - 2019 ARCAT, Inc. - All rights reserved

** NOTE TO SPECIFIER ** LP Building Products; engineered wood siding.
This section is based on the products of LP Building Products, which is located at:
414 Union St. Suite 2000
Nashville, TN 37219
Toll Free Tel: 888-820-0325
Fax: 877-523-7192
Email: request info (customer.support@lpcorp.com)
Web: https://lpcorp.com  
 [ Click Here ] for additional information.
People across the building industry tell us the LP name represents quality, dependability and consistency. Headquartered in Nashville, Tennessee, we are a leading manufacturer and distributor of building products. Founded in 1973, today we operate 26 manufacturing facilities in the U.S., Canada, Chile and Brazil.
We strive to deliver innovative, high-quality building products to retail, wholesale, home building and industrial customers. That's how we like it: we thrive on our reputation for ethics and teamwork - both internally and with our customers.

- GENERAL

  - SECTION INCLUDES

** NOTE TO SPECIFIER ** Delete items below not required for project.

    - Engineered Wood Siding/Cladding.

    - Soffit Panels.

    - Trim and Fascia.

    - Accessories:

      - Fasteners.

      - Sealant.

      - Water-resistive barrier.

      - Flashing.

  - RELATED SECTIONS

** NOTE TO SPECIFIER ** Delete any sections below not relevant to this project; add others as required.

    - Section 06 05 73.13 - Fire-Retardant Wood Treatment.

    - Section 06 10 00 - Rough Carpentry.

    - Section 06 20 00 - Finish Carpentry.

    - Section 07 62 00 - Sheet Metal Flashing and Trim.

  - REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

    - ASTM International (ASTM):

      - ASTM A 153 - Standard Specification for Zinc Coating (Hot-Dip) on Iron and Steel Hardware.

      - ASTM C 920 - Standard Specification for Elastomeric Joint Sealants.

    - American National Standards Institute (ANSI):

      - ANSI A135.6 - Engineered Wood Siding.

    - APA - The Engineered Wood Association (APA):

      - PS 2-10 - Performance Standard for Wood-Based Structural-Use Panels.

      - PRP 108 - Performance Standards and Qualification Policy for Structural-Use Panels.

      - PR-N124 - APA Product Report, LP SmartSide Strand Substrate Lap and Panel Siding.

      - PR-N117 - APA Product Report, LP SmartSide Strand Substrate Soffit.

    - Department of Housing and Urban Development (HUD):

      - HUD-MR-1318 - Material Release.

      - HUD-UM-40 - HUD Building Product Standards and Certification Program Plywood and Other Performance Rated Wood-Based Structural-Use Panels.

    - Florida Product Approval (FL#):

      - FL# 9190 - LP SmartSide Strand & Fiber Substrate Lap and Panel Siding.

      - FL# 9103 - LP SmartSide Strand & Fiber Substrate Lap and Panel Siding.

    - ICC Evaluation Service (ICC-ES):

      - ESR-1301 - LP SmartSide Strand Substrate Lap and Panel Siding.

      - ESR-3090 - LP SmartSide Fiber Substrate Lap and Panel Siding.

    - Texas Department of Insurance (TDI):

      - EC-22 - LP SmartSide Strand Substrate Lap and Panel Siding.

      - EC-35 - LP SmartSide Fiber Substrate Lap and Panel Siding.

    - Canadian Construction Materials Centre (CCMC):

      - CCMC # 11826-L - LP SmartSide Strand Substrate Lap and Panel Siding.

      - CCMC # 12353-L - LP SmartSide Fiber Substrate Lap and Panel Siding.

      - CCMC # 07893-L - LP CanExel Siding.

    - California Department of Forestry & Fire Protection - Office of State Fire Marshal - Fire Engineering - Building Materials Listing Program (BML):

      - BML No. 8140-2027:0001 - LP SmartSide Strand Substrate Lap Siding.

      - BML No. 8140-2027:0002 - LP SmartSide Strand Substrate Panel Siding.

      - BML No. 8140-2027:0003 - LP SmartSide Fiber Substrate Lap Siding.

      - BML No. 8140-2027:0004 - LP SmartSide Fiber Substrate Panel Siding.

  - SUBMITTALS

    - Submit under provisions of Section 01 30 00 - Administrative Requirements.

    - Product Data:

      - Application Instructions.

      - Maintenance and Care Instructions.

    - Verification Samples: For each exposed product and texture specified, two samples, minimum size 6 inches (152 mm) long representing actual product, color, and patterns.

    - Shop Drawings: Include details of materials, construction and finish. Include relationship with adjacent construction.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with a minimum five years documented experience.

    - Installer Qualifications: Company specializing in performing Work of this section with minimum two years documented experience with projects of similar scope and complexity.

    - Source Limitations: Provide each type of product from a single manufacturing source to ensure uniformity.

** NOTE TO SPECIFIER ** Include mock-up if multi-family or light-commerical project. The following is one example of how a mock-up on might be specified. When deciding on the extent of the mock-up, consider all the major different types of work on the project. Delete if single-family dwelling

    - Mock-Up: Construct a mock-up with actual materials in sufficient time for Architect's review and to not delay construction progress. Locate mock-up as acceptable to Architect and provide temporary foundations and support.

      - Intent of mock-up is to demonstrate quality of workmanship and visual appearance.

      - If mock-up is not acceptable, rebuild mock-up until satisfactory results are achieved.

      - Retain mock-up during construction as a standard for comparison with completed work.

      - Do not alter or remove mock-up until work is completed or removal is authorized.

  - PRE-INSTALLATION CONFERENCE

    - Convene a conference approximately two weeks before scheduled commencement of the Work. Attendees shall include Architect, Contractor and trades involved. Agenda shall include schedule, responsibilities, critical path items and approvals.

  - DELIVERY, STORAGE, AND HANDLING

    - Store and handle in strict compliance with manufacturer's written application instructions and recommendations.

    - Protect from damage due to weather, excessive temperature, and construction operations.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results. Do not install products under environmental conditions outside manufacturer's recommended limits.

  - SEQUENCING

    - Ensure that products of this section are supplied to affected trades in time to prevent interruption of construction progress.

  - WARRANTY

    - Manufacturer's Warranty: Provide manufacturer's Limited Warranty.

      - Limited Warranty Period: Fifty years, first 5 years equal to the cost of repairing or replacing, then prorated from the 6th year through the 49th year from the date of installation.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: LP Building Products, which is located at: 414 Union St. Suite 2000; Nashville, TN 37219; Toll Free Tel: 888-820-0325; Fax: 877-523-7192; Email: request info (customer.support@lpcorp.com); Web: https://lpcorp.com

** NOTE TO SPECIFIER ** Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

    - Substitutions: Not permitted.

    - Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 - Product Requirements.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - ENGINEERED WOOD SIDING/CLADDING

** NOTE TO SPECIFIER ** Delete basis of design options not required.

    - Basis of Design: Strand Panel Siding; as manufactured by LP Building Products.

      - Description: Exterior-grade, phenolic resin-saturated, paper overlay laminated to EPA-registered zinc-borate preservative-treated engineered wood siding. Exposed edges sealed for moisture resistance.

      - Finish: Acrylic latex primer.

** NOTE TO SPECIFIER ** Delete thickness options not required.

      - Thickness, 38 Series: 0.315 inch (8 mm) minimum.

      - Thickness, 76 Series: 0.375 inch (10 mm) minimum.

      - Thickness, 190 Series: 0.530inch (14 mm) minimum.

      - Style : Embossed Cedar Texture

** NOTE TO SPECIFIER ** Delete groove options not required.

      - Grooves: Channel grooves at 4 inches (102 mm) on center.

      - Grooves: Channel grooves at 8 inches (203 mm) on center.

      - Grooves: None.

** NOTE TO SPECIFIER ** Delete length options not required.

      - Length: 6 feet (1829 mm).

      - Length: 7 feet (2134 mm).

      - Length: 8 feet (2438 mm).

      - Length: 9 feet (2743 mm).

      - Length: 10 feet (3048 mm).

      - Length: 12 feet (3658 mm).

      - Width: 48 inches (1219 mm), nominal.

      - Edges: Shiplap.

    - Basis of Design: Strand Vertical Siding; as manufactured by LP Building Products.

      - Description: Exterior-grade, phenolic resin-saturated, paper overlay laminated to EPA-registered zinc-borate preservative-treated engineered wood siding. Edges beveled and sealed for moisture resistance.

      - Finish: Acrylic latex primer.

      - Thickness, 38 Series: 0.315 inch (8 mm) minimum.

      - Style: Embossed Cedar Texture.

      - Length: 16 feet (4877 mm).

      - Width: 16 inches (406 mm), nominal.

    - Basis of Design: Strand Lap Siding; as manufactured by LP Building Products.

      - Description: Exterior-grade, phenolic resin-saturated, paper overlay laminated to EPA-registered zinc-borate preservative-treated engineered wood siding. Edges beveled ad sealed for moisture resistance.

      - Finish: Acrylic latex primer.

** NOTE TO SPECIFIER ** Delete thickness option not required.

      - Thickness, 38 Series: 0.315 inch (8 mm) minimum.

      - Thickness, 76 Series: 0.375 inch (10 mm) minimum.

      - Style: Embossed Cedar Texture.

** NOTE TO SPECIFIER ** Delete width options not required.

      - Width: 5 inches (127 mm), nominal.

      - Width: 6 inches (152 mm), nominal.

      - Width: 7 inches (178 mm), nominal.

      - Width: 8 inches (203 mm), nominal.

      - Width: 9-1/2 inches (241 mm), nominal.

      - Width: 12 inches (305 mm), nominal.

      - Length: 16 feet (4877 mm).

      - SmartLock Cedar Texture, Size: 8 inches (203 mm) nominal width, 0.375 inch (10 mm) minimum thickness.

    - Basis of Design: Fiber Panel Siding, 76 Series; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Standards Compliance:  ANSI A135.6 compliant.

      - Finish: Acrylic latex primer.

      - Thickness: 0.375 inch (10 mm), minimum.

** NOTE TO SPECIFIER ** Delete style options not required.

      - Style: Reverse board and batten, 12 inch (305 mm) on center groove.

      - Style: Smooth Finish.

      - Style: Smooth Finish, 8 inch (203 mm) on center groove.

      - Style: Stucco Texture.

      - Style: Cedar Texture, 8 inch (203 mm) on center groove.

      - Style: Cedar Texture with square edge.

      - Width: 48.56 inches (1233 mm), actual width.

** NOTE TO SPECIFIER ** Delete length option not required.

      - Length: 8 feet (2438 mm).

      - Length: 9 feet (2743 mm).

      - Edges: Shiplap and Square Edge.

    - Basis of Design: Fiber Lap Siding, 76 Series; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Standards Compliance:  ANSI A135.6 compliant.

      - Finish: Acrylic latex primer.

      - Thickness, 76 Series: 0.375 inch (10 mm) minimum.

** NOTE TO SPECIFIER ** Delete style options not required.

      - Style: Smooth Finish.

      - Style: Cedar Texture.

      - Style: Colonial Beaded Smooth Finish.

      - Style: Colonial Beaded Sequoia Texture.

** NOTE TO SPECIFIER **  Delete width option not required

      - Width: 8 inches (203 mm) nominal.

      - Width: 9 inches (229 mm) nominal.

      - Length: 16 feet (4877 mm).

    - Basis of Design: Fiber Lap Siding, 120 Series; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Standards Compliance:  ANSI A135.6 compliant.

      - Finish: Acrylic latex primer.

      - Thickness, 120 Series: 0.450 inch (11 mm) minimum.

** NOTE TO SPECIFIER ** Delete style options not required.

      - Style: 12 inch (305 mm) nominal, Triple 4 inch (102 mm) Bold Profile.

      - Style: 12 inch (305 mm) nominal, Double 5 inch (127 mm) Bold Profile.

      - Style: 16 inch (406 mm) nominal, Quad 4 inch (102 mm) Bold Profile.

      - Style: 16 inch (406 mm) nominal, Triple 5 inch (127 mm) Bold Profile.

      - Style: 16 inch (406 mm) nominal, Double 8 inch (203 mm) Bold Profile.

** NOTE TO SPECIFIER **  Delete width options not required.

      - Width: 6 inches (152 mm) nominal.

      - Width: 8 inches (203 mm) nominal.

      - Width: 8 inches (203 mm) nominal, Self-Aligning Cedar Texture.

      - Width: 9.5 inches (241 mm) nominal.

      - Width: 12 inches (305 mm) nominal.

      - Width: 16 inches (406 mm) nominal.

      - Length: 16 feet (4877 mm).

    - Basis of Design: Fiber Cedar Shakes; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Standards Compliance:  ANSI A135.6 compliant.

      - Finish: Acrylic latex primer.

      - Thickness: 0.375 inch (10 mm), minimum.

      - Style: Cedar Texture with staggered edge or straight edge.

      - Size: 12 x 48 inches (305 x 1219 mm).

      - Edges: Shiplap Edge.

** NOTE TO SPECIFIER ** Delete Article if not required.

    - Basis of Design: Fiber Perfection Shingle; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Standards Compliance:  ANSI A135.6 compliant.

      - Finish: Acrylic latex primer.

      - Thickness: 0.375 inch (10 mm), minimum.

      - Style: Fine sawn wood texture with no knots and straight edge.

      - Size: 8 x 48 inches (203 x 1219 mm).

      - Edges: Shiplap Edge.

** NOTE TO SPECIFIER ** Delete Article if not required.

  - SOFFIT PANELS

** NOTE TO SPECIFIER ** Delete basis of design options not required.

    - Basis of Design: Strand Soffit ; as manufactured by LP Building Products.

      - Type: Exterior-grade, phenolic resin-saturated, paper overlay laminated to EPA-registered zinc-borate preservative-treated engineered wood soffit.

      - Finish: Acrylic latex primer.

      - Square edges.

** NOTE TO SPECIFIER ** Delete thickness options not required.

      - Thickness: 0.315 inch (8 mm) minimum.

      - Thickness: 0.375 inch (10 mm) minimum.

      - Thickness: 0.530 inch (14 mm) minimum.

      - Style : Cedar Texture.

** NOTE TO SPECIFIER ** Delete type options not required.

      - Type: Non-vented soffit.

      - Type: Non-vented, Cut-to-Width soffit.

      - Type: Vented, Cut-to-Width soffit.

** NOTE TO SPECIFIER ** Delete width options not required.

      - Width: 12 inches (305 mm), nominal.

      - Width: 16 inches (406 mm), nominal.

      - Width: 24 inches (610 mm), nominal.

      - Width: 48 inches (1219 mm), nominal.

** NOTE TO SPECIFIER ** Delete length option not required.

      - Length: 8 feet (2438 mm).

      - Length: 9 feet (2743 mm).

      - Length: 16 feet (4877 mm).

    - Basis of Design: Fiber Soffit ; as manufactured by LP Building Products.

      - Type: Engineered wood siding with resin and linseed oil impregnated surface, treated with EPA-registered zinc-borate preservative.

      - Finish: Acrylic latex primer.Square edges.

      - Thickness: 0.375 inch (10 mm).

** NOTE TO SPECIFIER ** Delete style option not required.

      - Style: Cedar Texture.

      - Style: Smooth Finish.

** NOTE TO SPECIFIER **  Delete type option not required

      - Type: Non-vented soffit.

      - Type: Non-vented, Cut-to-Width soffit.

** NOTE TO SPECIFIER ** Delete width option not required.

      - Width: 16 inches (405 mm).

      - Width: 47.94 inches (1218 mm) actual.

** NOTE TO SPECIFIER ** Delete length options not required.

      - Length: 8 feet (2438 mm).

      - Length: 9 feet (2743 mm).

      - Length: 16 feet (4877 mm).

** NOTE TO SPECIFIER ** Delete Article if not required.

  - TRIM AND FASCIA

** NOTE TO SPECIFIER ** Delete trim and fascia products not required.

    - Basis of Design: Strand Trim and Fascia; as manufactured by LP Building Products.

** NOTE TO SPECIFIER ** Delete subparagraph below if fire rating is not required.

      - Fire Rating: Class 1(A) fire rating required.

      - Finish: Acrylic latex primer.

** NOTE TO SPECIFIER ** Delete thickness options not required.

      - Thickness, 190 Series: 0.530 inch (14 mm).

      - Thickness, 440 Series: 0.625 inch (16 mm).

      - Thickness, 540 Series: 0.910 inch (23 mm).

      - Style : Cedar Texture.

** NOTE TO SPECIFIER ** Delete width options not required.

      - Width: 1.50 inches (38 mm), actual.

      - Width: 2.50 inches (64 mm), actual.

      - Width: 3.50 inches (89 mm), actual.

      - Width: 4.50 inches (114 mm), actual.

      - Width: 5.50 inches (140 mm), actual.

      - Width: 7.21 inches (183 mm), actual.

      - Width: 9.21 inches (234 mm), actual.

      - Width: 11.21 inches (285 mm), actual.

      - Length: 16 feet (4877 mm).

    - Basis of Design: Fiber Trim and Fascia; as manufactured by LP Building Products.

** NOTE TO SPECIFIER ** Delete subparagraph below if fire rating is not required.

      - Fire Rating: Class 1(A) fire rating required.

      - Finish: Acrylic latex primer.

** NOTE TO SPECIFIER ** Delete thickness option not required.

      - Thickness, 440 Series: 0.625 inch (16 mm) minimum.

      - Thickness, 540 Series: 0.910 inch (23 mm) minimum.

      - Style : Reversible; Smooth Finish on one side and Cedar Texture on the other side.

** NOTE TO SPECIFIER ** Delete width options not required.

      - Width: 2.70 inches (69 mm), actual.

      - Width: 3.50 inches (89 mm), actual.

      - Width: 4.50 inches (114 mm), actual.

      - Width: 5.50 inches (140 mm), actual.

      - Width: 7.21 inches (183mm), actual.

      - Width: 9.21 inches (234 mm), actual.

      - Width: 11.21 inches (285 mm), actual.

      - Length: 16 feet (4877 mm).

** NOTE TO SPECIFIER ** Delete Article if not required.

  - ACCESSORIES

** NOTE TO SPECIFIER ** Delete paragrpaphs not required.

    - Fasteners: ASTM A 153:

      - Hot-dip galvanized or stainless steel nails with 0.113 inch (2.9 mm) diameter shank.

      - Penetrate structural framing or wood structural panels and structural framing a minimum of 1-1/2 inches (38 mm).

    - Sealant: ASTM C 920, minimum Class 25 sealant.

    - Water-Resistive Barrier: ASTM D226 or other approved water-resistive barrier.

    - Air Barrier:

      - Material: ASTM E 1677 .

      - UV Exposure: Minimum three months.

      - Seam Tape: Air barrier manufacturer's standard product.

** NOTE TO SPECIFIER ** Include non-compressible drainable housewrap as water-resistive barrier for vertical siding or lap siding installed vertically installations. Delete if not required.

    - Non-Compressible Drainable Housewrap :

      - Non-Compressible: will not allow the minimum 1 mm drainage gap to be reduced by the force of fastening during the installation of siding.

      - Drainable Housewrap: will remove more bulk water by creating a minimum 1 mm drainage gap (air gap) at any individual measurement point between the housewrap and the back of the siding.

    - Flashing:

      - Provide flashing at window and door heads and where indicated on Drawings. Refer to Division 07 for sheet metal flashing.

** NOTE TO SPECIFIER ** Delete material options not required.

      - Material: Aluminum.

** NOTE TO SPECIFIER ** Delete finish options not required.

        - Finish: Siliconized polyester coating.

        - Finish: High-performance organic finish.

        - Finish: Factory-prime coating.

        - Finish: _______________________.

        - Finish: As determined by the Architect.

      - Material: Stainless steel.

      - Material: Galvanized steel.

      - Material: _______________________.

      - Material: As determined by the Architect.

- EXECUTION

  - EXAMINATION

    - Do not begin installation until substrates have been properly constructed and prepared.

    - If substrate preparation is the responsibility of another installer, notify Architect in writing of unsatisfactory preparation before proceeding.

    - Verify location of concealed framing support and anchorage.

  - PREPARATION

    - Clean surfaces thoroughly prior to installation.

    - Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

  - INSTALLATION

    - Install in accordance with manufacturer's application instructions approved submittals and in proper relationship with adjacent construction.

      - Install in accordance with conditions stated in ICC-ES ESR-1301 for strand substrate products and ICC-ES ESR-3090 for fiber substrate products.

      - Properly space joints to allow for equilibration.

    - Do not install over damaged or crooked materials.

    - Do not cut siding/cladding to fabricate trim; use trim components.

    - After installation, seal and flash joints, except the overlapping horizontal lap joints.

    - Seal around penetrations.

    - All wood substrate that is exposed to the weather must be sealed in a manner that prevents moisture intrusion and water build up.

      - Seal ALL exposed cuts of siding and trim. Field spray applied coatings on cuts are not recommended.

      - Sealing can be accomplished by applying a coating or sealant according to the manufacturer's requirements.

      - Butt joints that are covered with joint moldings, sealant, or factory prefinished ends are considered sealed from the weather.

  - CLEANING AND PROTECTION

    - Clean products in accordance with the manufacturers Care and Maintenance Instructions.

    - Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION